| NTC Thermistors |  |
| --- | --- |

Category; Type; Style; Resistance Range (Ohm); Reference Temp. (); Resistance Tolerance (%); B Constant; B Constant Tolerance (%); Temp. Range (); PDF. NTC thermistors; NT73; SMD; 1k 150k; 25; 5, 10, 15; 3200K 4100K; 3, 5, 10; −55 +125.

|  | PTC Thermistors |  |
| --- | --- | --- |

Category; Type; Style; Resistance Range (Ohm); Reference Temp. (); Resistance Tolerance (%); CurieTemp.; Temp. Range (); PDF. PTC thermistors; PT72; SMD; 50 1k; 25; 50; 70,80,100; −55 +125.

|  | Linear P.T.C. Resistors/Thick film |  |
| --- | --- | --- |

Category; Type; Style; Resistance Range (Ohm); Reference Temp. (); Resistance Tolerance (%); T.C.R.; Temp. Range (); PDF. Linear P.T.C. resistors/Thick film; LA73; SMD; 22 10k; 25; 5; 1000 3600 (×10−6/K); −55 +125.

|  | Linear P.T.C. Resistors/Thin film |  |
| --- | --- | --- |

Category; Type; Style; Resistance Range (Ohm); Reference Temp. (); Resistance Tolerance (%); T.C.R.; Temp. Range (); PDF. Linear P.T.C. resistorsThin film; LT73; SMD; 51 51k; 25; 2, 5; 150 4500 (×10−6/K); −40 +125. LT73V; SMD; 51 22k; 25; 2, 5; 150 4500 (×10−6/K); −55 +155. LP73; SMD; 100 10k; 25; 1, 2, 5; 3000 5000 (×10−6/K); −55 +125. MLT; MELF; 1k 9.1k; 25; 5; 2000 3900 (×10−6/K); −40 +125. LT; Leaded; 100 39k; 25; 5; 1000 4500 (×10−6/K); −40 +125. LP; Leaded; 1 100k; 25; 1, 2, 5; 150 5000 (×10−6/K); −55 +150.

|  | Platinum Thin Film Thermal Sensors |  |
| --- | --- | --- |

Category; Type; Style; Resistance range (Ohm); Reference temp. (); Resistance tolerance (%); T.C.R.; Temp. Range (); PDF. Platinum thin film thermal sensors; SDT73H; SMD; 100, 500; 0; 0.2, 1; 3850 (×10−6/K); −55 +155. SDT73V; −55 +155. SDT101A; Leaded; 10, 100, 500; 0, 25; 0.5, 1; 3500 (×10−6/K); −55 +150. SDT101B; −55 +300. SDT310LTC; Leaded; 100, 500, 1k; 0; 0.059 0.12, 0.39; 3850 (×10−6/K); −55 +155. SDT310P; −55 +400. SDT310MTM; 100; 0.12, 0.39; −55 +650. SDT310HLTC; 1k; 0.059 0.12, 0.39; −55 +155. SDT310AP; 10; 10; −55 +400. ST; Special form (custom); —; —; —; —; —. AFS; —; —; —; —; —.

Common Specification (Thermal Sensors). Items; PDF. Minimum Ordered Quantity. Recommended Pad Dimensions. Packagings For Chip Components. Axial Tapings. Color code•Resistance marking•E series numbers..